LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

Page n. 1

TECHNICAL DATA SHEET ART.CODE:  AN 1

NET MADE OF HIGH DENSITY POLYETHYLENE, KNOTTED, MESH mm 70 X 70 AND THICKNESS mm 5

STATIC TESTS: tests carried out on a polyethylene net, knotted, (braid Ø 5 mm circa and mesh mm 70) according to Standard EN 1263-1.

Hereafter the results obtained with tests on samples of a brand new net, dimensions 3 x  m:

AVERAGE ULTIMATE STRENGTH:   2493 daN

Technical features

- MATERIAL:  H.D. Polyethylene, stabilized against UV rays, water repellent.

- COLOR:  red or blue

- BRAID: Ø 5 mm, manufactured with 16 spindles + internal core (Titrage dtax)

- NET: squared mesh, knotted and thermo fixed.

- MESH:  mm 70 x 70 (according to Standard EN 1263-1 A2 – M100 – Q).

- EDGE STRIP: with a nylon rope with ultimate strength min.30 Kn

- WEIGHT: g. 400/sq m

LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Vertine, n. 7

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

Page n 2

TECHNICAL DATA SHEET ART.CODE:  AN 1

NET MADE OF HIGH DENSITY POLYETHYLENE, KNOTTED, MESH mm 70 X 70 AND THICKNESS mm 5

MATERIAL FEATURES: POLYETHYLENE

- SPECIFIC WEIGHT: 0,95 KG/DM2

- SOFTENING TEMPERATURE: 102° C

- FUSION TEMPERATURE: 120° C

- MIN. USE TEMPERATURE: – 40° C

- WATER ABSORPTION:  0,01% - WATER REPELLENT –

- MOTH RESISTANCE = ABSOLUTE

- MOULD RESISTANCE =  ABSOLUTE

- ABRASION RESISTANCE = EXCELLENT

- MINERAL ACIDS  = RESISTANT

- ORGANIC ACIDS  = RESISTANT

- BLEACHING SOLUTIONS = DAMAGED

- ALKALI = RESISTANT

- OIL = RESISTANT

- ORGANIC SOLVENTS = DAMAGED

All nets dimensions can be supplied on customer’s request, complete of their certification according to the EC standards EN 1263-1 and EN 1263-2. Nets are complete with a reinforced strip along the edge, eyelets at the angles for the hooking and the instruction manual for the installation.