LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

TECHNICAL DATA SHEET ART.CODE: A 15

NET MADE OF POLYETHYLENE, STABILIZED AGAINST UV RAYS, MESH mm 40 X 40 AND THICKNESS mm 2,2

BREAKING TEST:   tests carried out on a polyethylene net, without knot, green colored

(title 7/032 braid Ø mm. 2,2 and mesh mm 40).

Equipment used for the test on a sample with 5 meshes: dynamometer “Acquati model AG 5” with a max. carrying capacity of 5000 kg.

ELONGATION:    50%

ULTIMATE STRENGTH:   99 daN

Technical features

- MATERIAL:  H.D. Polyethylene, stabilized against UV rays, water repellent.

- AVAILABLE COLORS:  green

- YARN THICKNESS:  2,2 mm.

- NET: squared mesh

- MESH:  mm. 40 x 40

- WEIGHT: g. 80/sq m

- EDGE STRIP: with a 6 mm polyethylene braid

- FUSION TEMPERATURE: 120° C

- MIN. USE TEMPERATURE: – 40° C

- WATER ABSORPTION: 0,01% - WATER REPELLENT –

- MOTH RESISTANCE = ABSOLUTE

- MOULD RESISTANCE =  ABSOLUTE

- ABRASION RESISTANCE = EXCELLENT

- MINERAL ACIDS  = RESISTANT

- ORGANIC ACIDS  = RESISTANT

- ALKALI = RESISTANT

- OIL = RESISTANT

Each net can be manufactured with length and width on customer request. Nets are complete with a reinforced strip along the edge with a 6 mm braid sewed to the net. A piece of rope at the angles makes the installation easier.