LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

TECHNICAL DATA SHEET ART.CODE: A 18

NET MADE OF POLYETHYLENE, STABILIZED AGAINST UV RAYS, MESH mm 45 x 45, THICKNESS MM 3

STATIC TESTS: tests carried out with a polyethylene net, without knot, green colored (title 15/032,  braid Ø mm 3 and mesh mm 45) according to Standard EN 1263-1.

Hereafter the results obtained with tests on samples of a brand new net, dimensions 3 x 3:

AVERAGE ULTIMATE STRENGTH:   879 daN

Technical features

- MATERIAL:  High resistant Polyethylene, stabilized against UV rays, water repellent.

- AVAILABLE COLORS:  green or white

- YARN THICKNESS:  3 mm.

- NET: squared mesh

- MESH:  mm. 45 x 45

- WEIGHT: g. 120/sq. m

- EDGE STRIP: with a 6 mm polyethylene braid.

- FUSION TEMPERATURE: 120° C

- MIN. USE TEMPERATURE: – 40° C

- WATER ABSORPTION: 0,01% - WATER REPELLENT –

- MOTH RESISTANCE = ABSOLUTE

- MOULD RESISTANCE =  ABSOLUTE

- ABRASION RESISTANCE = EXCELLENT

- MINERAL ACIDS  = RESISTANT

- ORGANIC ACIDS  = RESISTANT

- ALKALI = RESISTANT

- OIL = RESISTANT

Each net can be manufactured with length and width on customer request. Nets are complete with a reinforced strip along the edge with a 6 mm braid sewed to the net. A piece of rope at the angles makes the installation easier.