LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

TECHNICAL DATA SHEET ART.CODE: A 25

NET MADE OF POLYETHYLENE, KNOTTED, STABILIZED AGAINST UV RAYS, MESH mm 40 x 40, THICKNESS MM 2.2

STATIC TESTS:  tests carried out on a polyethylene knotted net, green colored (title 3x7x600 denier and mesh mm. 40) according to Standard EN 1263-1.

Hereafter the results obtained with tests on samples of a brand new net, dimensions 3 x 3 m:

AVERAGE ULTIMATE STRENGTH:   854 daN

Technical features

- MATERIAL:  H.D. Polyethylene, stabilized against UV rays, water repellent.

- AVAILABLE COLORS:  green

- YARN THICKNESS:  2,2 mm.

- NET: squared mesh

- MESH:  mm. 40 x 40

- WEIGHT: g. 98/mq.

- EDGE STRIP: with a 6 mm polyethylene braid

- FUSION TEMPERATURE: 120° C

- MIN. USE TEMPERATURE: – 40° C

- WATER ABSORPTION: 0,01% - WATER REPELLENT –

- MOTH RESISTANCE = ABSOLUTE

- MOULD RESISTANCE =  ABSOLUTE

- ABRASION RESISTANCE = EXCELLENT

- MINERAL ACIDS  = RESISTANT

- ORGANIC ACIDS  = RESISTANT

- ALKALI = RESISTANT

- OIL = RESISTANT

Each net can be manufactured with length and width on customer request. Nets are complete with a reinforced strip along the edge with a 6 mm braid sewed to the net. A piece of rope at the angles makes the installation easier.