LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

Page n. 1

TECHNICAL DATA SHEET ART.CODE: A 28

NET MADE OF POLYETHYLENE, KNOTTED, STABILIZED AGAINST UV RAYS, MESH mm 20 X 20, THICKNESS mm  1,5

STATIC TESTS:   Tests carried out on a polyethylene knotted net, dark green colored (title Pe 3 x 4 x380 denier, mesh mm. 20 x 20).

Equipment used for the test: dynamometer “Acquati model AG 5” with a max. carrying capacity of 5000 daN.

Test carried out on a net with the following features: mg. 23 x mg. 23 and a sphere Ø 220 mm.

Load cell:   5.000 daN

Graphic scale:  40%

RESULTS:

ULTIMATE STRENGTH:   365 daN

Elongation: 35%

Technical features

- MATERIAL:  H.D. Polyethylene, stabilized against UV rays, water repellent.

- AVAILABLE COLORS:  green or black

- YARN THICKNESS:  1,5  mm.

- NET: squared mesh

- MESH:  mm. 20 x 20

- WEIGHT: g. 95/Sq m

- EDGE STRIP: with a 6 mm polyethylene braid

- FUSION TEMPERATURE: 120° C

- MIN. USE TEMPERATURE: – 40° C

- WATER ABSORPTION: 0,01% - WATER REPELLENT –

Pag. n. 2

- MOTH RESISTANCE = ABSOLUTE

- MOULD RESISTANCE =  ABSOLUTE

- ABRASION RESISTANCE = EXCELLENT

- MINERAL ACIDS  = RESISTANT

- ORGANIC ACIDS  = RESISTANT

- ALKALI = RESISTANT

- OIL = RESISTANT

Each net can be manufactured with length and width on customer request. Nets are complete with a reinforced strip along the edge with a 6 mm braid sewed to the net. A piece of rope at the angles makes the installation easier.