LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

TECHNICAL DATA SHEET ART.CODE:  A 44

NET MADE OF POLYETHYLENE, MESH mm 45 x 45, THICKNESS mm 5

STATIC TESTS: tests carried out on a 3D net, made of high resistant polyprophilene, stabilized against UV rays, without knot, green colored, (title 15000 denier, mesh mm 45 x 45) according to Standard EN 1263-1, par. 7.7.

Hereafter the results obtained with tests on samples of a brand new net, dimensions 3 x 3 m:

AVERAGE ULTIMATE STRENGTH:   2446 daN

Technical features

- MATERIAL:  H.D. Polyethylene

- AVAILABLE COLORS:  green

- YARN THICKNESS:  5 mm.

- NET: squared mesh

- MESH:  mm 45 x 45

- WEIGHT: g. 500/sq m

- EDGE STRIP: with a 6 mm polyethylene braid

Each net can be manufactured with length and width on customer request. Nets are complete with a reinforced strip along the edge with a 6 mm braid sewed to the net. A piece of rope at the angles makes the installation easier.