LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

TECHNICAL DATA SHEET ART.CODE:  A 45

NET MADE OF H.D. POLYETHYLENE, KNOTTED, MESH mm 50 X 50 AND THICKNESS mm 4

STATIC TESTS: tests carried out on a polyethylene net, knotted, light green colored, braid Ø 4 mm and mesh mm 50,  according to Standard EN 1263-1, par. 7.7

Hereafter the results obtained with tests on 3 samples of a brand new net, dimensions 3 x 3 m:

AVERAGE ULTIMATE STRENGTH:   2186 daN

Technical features

- MATERIAL:  H.D. Polyethylene, stabilized against UV rays, water repellent.

- AVAILABLE COLORS:  green

- YARN THICKNESS:  4  mm

- NET: squared mesh

- MESH:  mm. 50 x 50

- WEIGHT: g. 420/sq m

- EDGE STRIP: with a 6 mm polyethylene braid.

- FUSION TEMPERATURE: 120° C

- MIN. USE TEMPERATURE: – 40° C

- WATER ABSORPTION: 0,01% - WATER REPELLENT –

- MOTH RESISTANCE = ABSOLUTE

- MOULD RESISTANCE =  ABSOLUTE

- ABRASION RESISTANCE = EXCELLENT

- MINERAL ACIDS  = RESISTANT

- ORGANIC ACIDS  = RESISTANT

- ALKALI = RESISTANT

- OIL = RESISTANT

Each net can be manufactured with length and width on customer request. Nets are complete with a reinforced strip along the edge with a 6 mm braid sewed to the net. A piece of rope at the angles makes the installation easier.