LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

TECHNICAL DATA SHEET ART.CODE: AN 2

NET MADE OF HIGH RESISTANT NYLON, MESH mm 50 x 50, THICKNESS mm 5

STATIC TESTS: carried out on a nylon polyamide 6 (210/180) net, without knot, white colored (braid Ø5mm and mesh mm 50) according to Standard EN 1263 – 1

Hereafter the results obtained with tests on samples of a brand new net, dimensions 3 x 3m:

AVERAGE ULTIMATE STRENGTH:   2720,5 daN

Technical features

- MATERIAL:  Nylon polyamide 6 title 210/180 without knot

- AVAILABLE COLORS:  white

- YARN THICKNESS:  5 mm.

- NET:  squared mesh

- MESH:  mm 50 x 50

- WEIGHT: g. 390/ sq m

- EDGE STRIP:  with a high resistant 10 mm nylon braid,  sewed to the net. A piece of rope at the angles makes the installation easier.

- DIMENSIONS: on request.