LABORATORIO ARTIGIANO RETI

di ARCHETTI CARLO

Reti da Pesca – Sport – Caccia

Recinzione Impianti Sportivi

Antinfortunistica – Acquacoltura

25058 SULZANO  (BS) – Via Tassano, n. 8

Tel. e Fax 030/985290 – Tel. Ab. 030/985191

Cell. 328 0562071  c.f. RCHCRL64C01F532U – P.I. 03216410179

www.retiarchetti.it –  info@retiarchetti.it

www.retiarchetti.com – info@retiarchetti.com

TECHNICAL DATA SHEET ART.CODE: AN 3

NET MADE OF HIGH RESISTANT NYLON, MESH mm 42 x 42, THICKNESS mm 3

BREAKING TEST:   tests carried out on a nylon net, without knot, white colored (title 210/90 braid Ø mm 3 and mesh mm 42) according to Standard EN 1263-1.

Equipment used for the test on a sample with 5 meshes: dynamometer “Acquati model AG 5” with a max. carrying capacity of 5000 kg.

ELONGATION: 50%

ULTIMATE STRENGTH:   290 daN

Technical features

- MATERIAL:  Nylon polyamide 6, title 210/90, without knot.

- AVAILABLE COLORS:  white

- YARN THICKNESS:  3 mm.

- NET: squared mesh

- MESH:  mm. 42 x 42

- WEIGHT: g. 215/Sq m

- EDGE STRIP: with a 8 mm high resistant nylon braid.

Each net can be manufactured with length and width on customer request. Nets are complete with a double reinforced strip along the edge with a 8 mm braid sewed to the net. A piece of rope at the angles makes the installation easier.